LOCKPILE  COCOA

| Product Specification Sheet |  |  |
| --- | --- | --- |
| PROPERTY | SPECIFICATION | TEST METHOD |
| Product | Nonwoven Thermal Bond Carpet |  |
| Application | Miscellaneous Trim Applications |  |
| Construction | 100% Recycled, 87% Solution Dyed Polypropylene, 13% Polyethylene Binder Fibre, 15-20 denier x 6.35cm – 8.89cm Staple with 5-7 denier x 3.81cm – 6.35cm Binder Fibre |  |
| Weight | 482gsm +/- 25gsm | ASTM D3776-96 Option A |
| Width | 1.95m |  |
| Thickness | Approximately 5.0mm |  |
| Breaking Strength | MD 34.02kg min AMD 38.56kg min | ASTM D1682 Grab Method |
| Pile Height | 2.0mm +/- 0.75mm |  |
| Colour | Cocoa | Visual |
| Appearance | Random Needled | Visual |
| Flammability | Will meet requirements on a stand alone basis If laminated to a substrate must be tested as a composite | FMVSS-302 |
| Date Revised | 26th October 2016 |  |