LOCKPILE  (ALL COLOURS EXCEPT COCOA)

| Product Specification Sheet |  |  |
| --- | --- | --- |
| PROPERTY | SPECIFICATION | TEST METHOD |
| Product | Nonwoven Thermal Bond Carpet |  |
| Application | Miscellaneous Trim Applications |  |
| Construction | 100% Recycled, Solution Dyed Polyester Nonwoven Material with Latex Back Coating |  |
| Weight | 484.85gsm +/- 50.86gsm | FTM NW508 ASTM D3776 |
| Width | 1.83m | FTM NW502 ASTM D3774 |
| Thickness | 5.72mm +/- 1.02mm | FTM NW504 ASTM D5729 |
| Tensile Strength | MD 45.36kg min CMD 54.43kg min | FTM NW505 ASTM D5034 |
| Elongation at 11.34kg (Instron) | MD 12% max CMD 8% max | FTM NW506 ASTM D5034 |
| Pile Height | 5.0mm +/- 0.5mm | FTM NW523 |
| Colour | Beige, Mocha, Wine, Navy, Ash Grey, Coal, Charcoal, Cinder, Black | Visual |
| Appearance | Match Approved Standard | Visual |
| Date Revised | 26th October 2016 |  |